## Slide 1: Promising Directions for Developing Nano-structured Photocathodes
Michael Pellin
Argonne Distinguished Fellow
Director, Materials Science Division
Thomas Prolier, Jeff Elam, Alex Martinson
Stacey Standridge (NU), Joe Hupp (NU)
1st Workshop on Photo-cathodes: 300nm-500nm
July 20-21, 2009: University of Chicago

## Slide 2: Outline
Issues Arising
Atomic Layer Deposition (Synthesis)
Barrier Layers
Layered Thin Films
Plasmon Enhanced Absorption

## Slide 3: Photocathode Issues
Conductivity
Balancing Absorption and Electron Collection
  Photon Absorption Lengths are long
    Nanostructuring
    Plasmonics
  Electron Diffusion Lengths are short

## Slide 4: Atomic Layer Deposition (ALD)
Layer-by-layer thin film synthesis method
Atomic level control over thickness and composition (even on very large areas)
Precise coatings on 3-D objects
Some unique possibilities for morphology control

## Slide 5: ALD Reaction Scheme
ALD involves the use of a pair of reagents.
  each reacts with the surface completely
  each will not react with itself
This setup eliminates line of site requirments
Application of this AB Scheme
  Reforms the surface
  Adds precisely 1 monolayer
Pulsed Valves allow atomic layer precision in growth
Viscous flow (~1 torr) allows rapid growth
  ~1 mm / 1-4 hours
0
500
1000
1500
2000
2500
3000
3500
4000
0
500
1000
1500
2000
2500
3000
AB Cycles
Thickness (Å)
Ellipsometry
Atomic Force Microscopy
Film growth is linear with AB Cycles
RMS Roughness = 4 Å (3000 Cycles)
ALD Films Flat, Pinhole free
Flat, Pinhole-Free Film
Seagate, Stephen Ferro
No uniform line of sight requirement!
Errors do not accumulate with film thickness.
mm’s in 1-3 hrs
Pinholes seem to be removed.
Single Cell, 9 cell, re-entrant, in situ

## Slide 6: ALD Thin Film Materials

## Slide 7: ZnO in Silicon High Aspect Ratio Trench
1 μm
200 nm
ZnO
Si
ALD is very good at coating non-planar surfaces

## Slide 8: Mixed Oxide Deposition: Layer by Layer
Mixed Layer Growth
Layer by Layer
note “steps”
atomic layer sequence “digitally” controlled
Films Have Tunable Resistivity, Refractive Index, Surface Roughness, etc.
[(CH3)3Al // H2O]
100 nm
ZnO
ZnO
Al2O3
Al2O3
[(CH3CH2)2Zn
// H2O]
Mixed Layers w/ atomic precision
Low Temperature Growth
Transparent
Uniform
Even particles in pores can be coated.

## Slide 9: ALD: Abrupt Semiconductor Dielectric Boundaries
Semiconductor Industry – a clue
  Silicon is reactive but oxide is simple and passivates well (but has a low dielectric constant)
  Gate dielectric oxides are now being used on Si
  metal (and being produced by ALD
  20 m2 / batch)
Si
HfO2
Epoxy

## Slide 10: Components of ALD System
Pump
Heated Substrates
Carrier Gas
Valves
Flow
Heaters
Reaction Chamber
N2
Flow
B
A
Precursors
Equipment is simple
Scale up is straightforward

## Slide 11
ALD Viscous Flow Reactors at ANL
10 chemical precursor channels
  gas, liquid, or solid
  precursor temperature to 300°C
  ozone generator
Reaction temperature to 500°C (1000°C)
In-situ measurements
  thickness (quartz microbalance)
  gas analysis (mass spectrometer)
Coat flat substrates (Si), porous membranes, powders, etc.

## Slide 12: Anodic Aluminum Oxide Membrane Properties
High Surface area substrates for increased absorption
Typical membrane properties
Membrane thickness = 75 mm
Conductance ~ 0.2 sccm/torr (N2 @ 1 atm)
Surface area of a single membrane ~ 0.05 m2
Histogram of particle diameters
obtained by image particle analysis
Pore Density 154 pores/mm2
FWHM 3.8 nm
Mean dia. 56 nm

## Slide 13: Combining AAO and ALD
Conformal deposition of a wide variety of metals and metal oxides
Extraordinary control over layer thickness
TiO2
TiO2
Al2O3 pore wall
pore

## Slide 14: AAO/ALD Electrode Design Incorporating Transparent Conducting Oxide (TCO)
Key feature:
w/o TCO  60 m
e- path thru semi-
conductor: longitudinal transport
with TCO  6 nm
e- path thru semi-
conductor: radial transport

## Slide 15: Enhanced Performance From Radial Charge Collection
Higher photocurrents (x20) with interdigitated TCO
Radial charge collection:
  Accelerates electron transport
  Reduces electron-hole recombination

## Slide 16: Plasmonic Photocathode Demonstration
Fig. 18. A schematic representation of field enhanced metal nanoparticle solar cell geometry is shown. In this design, serve only as plasmonic amplifiers. In future designs, interconnected particle arrays will also serve as current collectors, enabling the TCO to be omitted.
Figure 1. Plasmonic energy transfer scheme. Ag plasmonic absorbers are excited by the absorption of a photon. Excitation is short lived in a plasmon normally with internal conversion losing the excitation to heat in a few 10’s of fs.** In a solar cell, a second route to de-excitation of the plasmon is energy transfer to a nearby dye (k1). Rapidly this excitation results in electron transfer to the wide band gap semiconductor, k2, ( ~ 3 fs)* or intersystem crossing to a triplet dye state and then e transfer.

## Slide 17: Plasmonic Absorption Enhancement
Fig. 16. a) N719 dye on low-area (flat) TiO2 electrode, b) silver nanoparticle-coated, low-area (flat) TiO2 electrode, c) N719 dye on TiO2 (ALD)-coated silver nanoparticle layer on electrode. Quantitative measurements indicated ca. 5 to 7 fold enhancement in dye absorption in the presence of silver particles.
Fig.17. Plasmonic enhancement of photocurrent generation for a nominally flat photoelectrode featuring ALD coated (TiO2) silver nanoparticles as amplifiers. Currents are lowest with thick ALD coatings (little plasmon amplification) and highest with thin ALD coatings (substantial plasmon amplification).

## Slide 18
Combination Contact and Enahncer
Fig. 20. Interconnected metal particle arrays for combined light enhancement and electron collection. Schematic A) top view; b) side view, c) SEM image of a test Ag structure.

## Slide 19: Internal Stripes
Internal Stripe Deposition Concept
Objective : deposit specified surface species at arbitrary depths in the membrane. Several schemes are possible to achieve this:
In A, additional pore narrowing must be tolerated which is undesirable because the diffusion depth is a strong function of pore diameter.
Scheme B not effective for many subsequent ALD cycles; difficult to achieve complete passivation and inertness to oxidizer.
Masking Stripe
trimethyl aluminum exposure
Me
O
Al
O
O
O
O
O
O
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
Me
Al
Me
Al
Me
Al
Me
Al
Me
Al
Internal Stripe
diethyl zinc exposure
Me
O
Al
O
O
O
O
O
O
O
O
O
O
O
O
O
H
O
H
O
H
Me
Al
Me
Al
Me
Al
Me
Al
Me
Al
Et
Zn
Et
Zn
Et
Zn
Et
Zn
Et
Zn
Et
Zn
Oxidation
water exposure
O
Al
O
O
O
O
O
O
O
O
O
O
O
O
O
H
O
H
O
H
Al
Al
Al
Al
Al
Zn
Zn
Zn
Zn
Zn
Zn
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
O
H
d1
d1
d2
d (depth into pore from membrane surface)
Pore wall
Scheme A
Overcoating
Scheme C
Concurrent
2-stripe
growth
Scheme C:
This scheme is implemented in three steps:
1
2
3
ZnO
Al2O3
Scheme B
Permanent
Passivation
(silane treatment)
alkane
terminated

## Slide 20: Internal ZnO Stripes Positioning
0.5 sec
1.0 sec
1.5 sec
Depth Positioning
The TMA mask stripe depth was varied keeping all other growth parameters constant
Timing: 20c(x-5-4-10-5-15) (TMA-purge-DEZ-purge-H2O-purge)
The delay caused by the increasing depth of the passivating stripe causes a narrowing of the Zn stripe width.
Zn La

## Slide 21: Benefits of Argonne Nanostructured PV Technology
Lower manufacturing cost than other PV technologies
Non-vacuum, low temperature fabrication
Very tolerant to impurities (no clean room necessary) – light absorption and charge separation occur close to interface
Inexpensive, abundant, benign materials (e.g. TiO2, ZnO)
Robust nanoscale process