## Slide 1: In Situ Measurement Tools (for Monitoring and Understanding Photocathode Growth)
Second Workshop on Photocathodes: 300-500nm
June 29-30, 2012, Enrico Fermi Institute, University of Chicago
Jeffrey W. Elam
Argonne National Laboratory
Notes: 4

## Slide 2: Outline
Quantum yield (or photocurrent)
  Extremely relevant, but insight?...
Quartz crystal microbalance
Ellipsometry
X-ray methods
  Fluorescence
  Reflectivity
  Absorption

## Slide 3: In Situ QCM during Atomic Layer Deposition of In2O3
~0.01 ML sensitivity
Real time, in situ
Directly measures mass (ng/cm2)
Assume density to get film thickness
Reveals nucleation and growth regimes
Sensitive to temperature

## Slide 4: Island Growth (Volmer-Weber) Monitored by QCM
In situ QCM can reveal photocathode growth mode

## Slide 5: In Situ Measurements During ZnO-Al2O3 Alloy ALD
QCM shows removal of material during TMA exposures
QMS shows Zn(Me)2 during TMA exposures
Etching: ZnO + Al(Me)3 (g) → AlOMe + Zn(Me)2 (g)
QCM
QMS
QCM Can Reveal Surface Chemical Processes

## Slide 6: Temperature Sensitivity of QCM Crystals
(Assumed density = 3 g/cc)
QCM can be extremely sensitive to temperature
Temperature-compensated crystals help

## Slide 7: In Situ Spectroscopic Ellipsometry (SE)
TiN ALD
Sub-ML sensitivity
Insensitive to temperature
Can extract thickness, density, roughness, conductivity…
Model dependent
Useless for opaque films

## Slide 8: Modeling of Ellipsometric Data to Obtain Electrical Properties of Film

## Slide 9: X-ray Fluorescence
ZnO ALD

## Slide 10: X-Ray Reflectivity
ZnO ALD
Sub-ML sensitivity
Insensitive to temperature
Transparent or opaque filsm
Can extract thickness, density, roughness …
Model dependent

## Slide 11: In Situ X-Ray Absorption Spectroscopy During Pt ALD
W. Setthapun et. al., J. Phys. Chem. C, 114 (21), pp 9758–9771,(2010).
Pt Loading
Pt Bonding
XANES
Nearest Neighbors, Pt Particle Size
EXAFS
(Fourier Transform, Model)
Pt L3 edge

## Slide 12: X-Ray Absorption
Pt ALD
3K + Sb → 3K+ + Sb3-