## Slide 1
My take on the results from two cesiation trials

## Slide 2: First cesiation, Tile 10, Summer 2016
Second cesiation, Tile 13, Fall 2016
Oct 25
First cesium
exposure
Sept 30
Tile 13 Sealed
Nov 16
Tile 13
Flame Sealed!
July 11
Visual Cue of
Cesium having
Arrived on the
window
Aug 19
Tile 10
Flame Sealed!
Mar 31
Tile 10 sealed and taken out
of Margherita
Mar 26
G.P Review
June 27
Ampule broken
Seal = 0 days
Cesium exposure = @26 days
Flame seal = @48 days
Seal = 0 days
Open to air = @~70 days
Cesium exposure = @101 days
Flame sealed = @147 days

## Slide 3: Visual change tile 1
Before
After

## Slide 5: Visual change tile 2

## Slide 7: Guiding cesium through a straw into a small bathroom and condensing it on a vanity mirror
Tube is ~1/4’’ diameter
= 0.3 cm2 cross section
2x 8’’ MCPs
= ~8x104 cm2 S.A.
Antimony window
= 400 cm2 S.A.

## Slide 8: First tile
A few days go by in a saturated cesium environment
Before
After
Not totally conclusive, want more evidence of reaching the far end of the tile …

## Slide 9: Second tile
Hotter configuration: 190C instead of 140C on J-Tube

## Slide 10: What happens over long periods of time?
1) Photoresponse changes
2) Stack resistance changes

## Slide 14: Moving forward
More trials: we’ve only done two
Same or different procedure?
Better monitoring of QE (2D stage)
Understanding MCPs
New materials (K2CsSb)