## Slide 1: Visualizing Crystal Growth and Solid State Chemistry During the Recipe of bi-alkali photocathodes on Si(100)
Miguel Ruiz-Osés
Postdoc Stony Brook University
Contact: mruizoses@gmail.com
2nd Workshop Photocathodes, Chicago 06/30/2012

## Slide 2
Introduction:
Alkali antimonide cathodes are critical both for high-average current photoinjectors and for high quantum efficiency photodetectors.
Problems-Challenges:
Extreme vacuum sensitivity, non-reproducibility and poor lifetime.
Photoinjectors performance:
  QE of 2-6% at 532 nm and >10% at 355 nm
  QE unchanged at cryogenic temperature
  > 50 mA from 7 mm radius spot
  High Uniformity
  Emittance

## Slide 3
Correlation Between Material Properties and Performance
Study of the growth parameters, including both transparent and metallic substrates, sputtered and evaporated films, variation of growth time and temperatures and post-growth annealing processes. RECIPE
By means of these Techniques…
X-Ray Diffraction in-situ growth
XPS: Chemistry of growth
Techniques:
Effort to improve the performance of alkali antimonides ( K2CsSb) based on characterization of cathode formation during growth.

## Slide 4
Technique 1: XPS Chemistry of growth
wikipedia

## Slide 5
Center Functional Nanomaterials, CFN.
UHV system (5x10-10 Torr base pressure)
Heating/cooling substrate/cathode
Load lock (fast exchange of substrates)
Horizontal deposition of Sb, K and Cs.
Residual Gas Analizer RGA
Analyzer
Evaporator
STM/AFM

## Slide 6
Chemistry of the Sb reaction with alkalis:
Sb signature
Complete reaction of Sb with alkalis

## Slide 7
Temp dependence of Oxides
Oxides removal
Sb signature
QE(%)=1.2%
QE(%)=1%
Possible ex-situ preparation?

## Slide 8
Conclusions XPS:
Evidence of Sb reaction with alkalis
Alternative ex-situ preparation of Sb sputtered substrates which are cleaned by annealing.

## Slide 9
XRD: Atomic arrangement of materials.
Monochromatic X-Ray
Coherent X-Ray scattering = f( e- distribution in sample)
“The intensity and spatial distributions of the scattered X-rays form a specific
diffraction pattern which is the “fingerprint” of the sample.
monocrystaline
polycristaline
2D area detector
Techniques 2: XRD Crystalline structure during growth

## Slide 10
Horizontal evaporation of three sources:
140
25
T(C)
t
Sb
K
Cs
Recipe:
100
Experimental set up: K2CsSb cathodes growth
X-rays
Sb
K
Cs
FTM
P=1x10-10 mbar
QE(%)
t
K
Cs
QE during growth (532 nm laser)

## Slide 11
in-situ X-ray diff during deposition.
UHV system (2x10-10 Torr base pressure)
Residual Gas Analyzer (RGA)
Heating/cooling substrate/cathode
Load lock (fast exchange of substrates)
Horizontal deposition of Sb, K and Cs.
4 axis diffractometer UHV chamber
Beam Energy = 10 keV, λ = 1.2398 Å
Mono Resolution (ΔE/E) = ~ 2x10-4
Flux = ~ 2x1012 ph/sec @ 300 mA
Spot Size = ~ 1 x 0.5 mm2
nu - 2θ
(table)
Evaporators
zeta - θ
(sample)
X-rays
X21/NSLS Beamline
Portable chamber!
Camera 1
Camera 2
Two 2D detectors (Pilatus 100K):

## Slide 12
α: Swing angle
D: Distance sample-detector
XL, YL, ZL: Lab coordinates
ZL
XL
YL
1
2
D
α
X-rays
Diffractometer plane
  XRR movie while evaporation
  Theta-2theta scan WAXS
  (after evaporation)
Camera 1: Scan in diff plane

## Slide 13
ZL
XL
YL
1
α’
D’
X-rays
  XRD movie while evaporation
α’= 25˚
Diffractometer plane
Camera 2: Scan out of diff plane

## Slide 14
X-Ray reflectivity (XRR)
Wide Angle X Ray Scattering (WAXS)
  thickness of thin film layers
  density and composition of thin film layers
  roughness of films and interfaces
Camera 1
Camera 2
  phase composition (what phases are present)
  quantitative phase analysis- (how much of each phase is present)
  unit cell lattice parameters
  crystal structure
  average crystallite size of nanocrystalline samples
  crystallite microstrain
  texture
  residual stress (really residual strain)
FIXED ANGLE α
SCAN IN ANGLE
FIXED ANGLE α’
Wide Angle X Ray Scattering (WAXS)
Set of data
QE(%)
t
K
Cs
QE measurement during growth

## Slide 15: 165Å Sb at RT on Si(100)
0Å
165Å
time
14.9˚
39.3˚
Influence of the Sb structure on the growth of the cathode:
Correlation between structure of Sb and the final structure of the cathode?
Is the substrate having an influence in the Sb growth?
Is there a correlation between reactivity, QE and roughness?
Camera 1: XRR
Camera 2: WAXS
Sb peaks
(012)
(104)
(110)
(003)

## Slide 16: K at 140C
Camera 1
Camera 2
time
~10Å
~290Å
~495Å
~500Å
K3Sb peaks (K diffusion into Sb)
Sb peaks
(012)
(104)
(110)
(220)
(111)
(420)
2000 s
3800 s
4645 s
4697 s
QE(%)=0.1%

## Slide 17: Cs at 130C
0Å
25Å
763Å
0Å
901Å
Camera 1
Camera 2
time
QE(%)=1.4%
700s
1220s
4400s
5000s
700 s
1220 s
4400 s
5000 s
K2CsSb peaks
28˚
23.8˚
(111)
(220)
(420)
(200)
(220)
(222)
(400)
(331)
(420)
K3Sb peaks

## Slide 18: Cathodes comparison
Cathode2
QE(%)=0.4%
QE(%)=3.7%
100C
Cathode 1
Sb
K3Sb
K2CsSb
(012)
(104)
(110)
(003)
(111)
(220)
(420)
QE(%)=1.4%
QE(%)=0.1%
RT
RT vs 100C Sb evaporation: Starting configuration of Sb different in both cases.

## Slide 19: K3Sb formation:
Cathode 1
(012)
Cathode2
QE(%)=0.4%
QE(%)=0.1%
Camera 1
Camera 2
137Å
205Å
312Å
0s
1180s
1840s
2820s
K3Sb peaks
Sb peaks
Camera 1
Camera 2
time
~10Å
~290Å
~495Å
~500Å
2000 s
3800 s
4645 s
4697 s
1. Start K reaction
1
2
2. K is not initially sticking
3
3. Low intensity fringes and larger background= rougher surface enhanced reaction rate

## Slide 20: WAXS After evaporation
Cathode 1
K2CsSb
(012)
Cathode2
QE(%)=3.7%
QE(%)=1.4%
(200)
(220)
(222)
(400)
(222)
(220)
(200)
Cathode 2
(400)
Cathode 1
Fingerprints for QE improvement?
249Å Cs
756Å Cs
K2CsSb:

## Slide 21
Evidence of Sb effect on final QE performance.
K and Cs diffusion movies correlated to QE measurements.
Assignment of phases to QE improvement
QE degradation analysis related to crystalline phases amounts.
Low PH2O/PCO/PCO2 probed to be crucial.
Conclusions XRD:

## Slide 22
EDX : final Sb thickness: (36 nm cath 1, 40 nm cath 2).
In line with expected totals based on FTM values.
SEM and EDX after brief exposure to air
Segregation of K and uniform coverage of Cs and Sb:
(K forms islands during deposition or that air exposure preferentially removes K).
Sb and Cs were found in the correct stoichiometric ratio (~1:1), however a dearth of K was observed.
Microscopy:
UHV-AFM
QE(%)=1.1%
K2CsSb
SEM
EDX:Energy Dispersive X-rays

## Slide 23: Thanks to:
X. Liang, E. Muller, M. Gaowei, I. Ben-Zvi, Stony Brook University
J. Smedley, K. Attenkofer, Brookhaven National Lab
T. Vecchione , H. Padmore, Lawrence Berkeley Lab
S. Schubert, Helmhotlz Zentrum Berlin, Germany

## Slide 24
First Cathode
Full Cathode
QE(%)=1.4%
No cathode

## Slide 25
QE(%) 062012 532 nm = 1.2
QE(%) 062112 532 nm = 1.8
Spectral Response