## Slide 1: Speed-I View from Material Side
Qing Peng, Anil U. Mane, Jeffrey W. Elam
Energy Systems Division
Argonne National Laboratory
Limitations on Fast Timing Workshop at U of Chicago

## Slide 2: Components Contribute to Timing of MCP detector
V1
V2
V4
V3
V5
t1
t2
t3
t4
t5
Photocathode
Microchannel plate
Anode
Rev. Sci. Instrum. 81, 073112 (2010)

## Slide 3: Transition Time Spread AND Transition Time
m: Electron Mass
v0: Initial speed of electron
v: Final speed of electron
∆V: Voltage different between collision
L
Nuclear instruments and methods, 162 (1979), 587-601.
e
νv
νι
D
Transition time
Rise time and Transition time spread
related to spread of Vι

## Slide 4: What determines timing?
The Transition time spread
  Proportional to L, for given L/D and voltage
  Proportional to transition time, for given L/D and voltage
  Smaller D, Smaller FWHM
  Smaller distribution of Vι,(smooth wall surface of MCP), Smaller FWHM
The transition time
  Proportional to channel length (L)
  Space charge saturation set a standard L
  Well defined repeatable the transition time
So Timing is a strong function of channel length, given
L/D and potential and other parameters fixed Operated in saturation range
L
Nuclear instruments and methods, 162 (1979), 587-601.
e
D
νv
νι

## Slide 5: What determines the Length of MCP for operating in saturation region
G: gain
α: Length to diameter ratio
αm: L/D when Gain is saturated, normally
αm ~ 40-60
V: Total channel voltage
A: constant
V0: initial energy of an emitted 2nd electron
(~1eV)
L/D of MCP for saturated gain: 40-60
L is determined by D
Smaller D, Smaller L, faster timing
D has been reported down to 2μm
Nuclear instruments and methods, 162 (1979), 587-601.
S. Tremsina etc, Proc. SPIE, vol. 4854
B. N. Laprade etc, Proc. SPIE 3173, pp. 474-485 (1997)

## Slide 6: What determines the Length of MCP for operating in saturation region
G: Gain
δ (1) to δ (n): Secondary electron
Coefficient during 1 to n strike on channel
Since Gain of MCP has upper limit (~104) due to ion feedback and performance instabilities
Larger δ, will give smaller L
Smaller L, faster timing
Nuclear instruments and methods, 162 (1979), 587-601.

## Slide 7: Several Thoughts for Faster Timing from Material View
MCPs with smaller pore size
Engineering the Pore Entrance
Engineering the SEE material inside of pore
Decrease Ion feedback

## Slide 8
Al
CH3
CH3
CH3
OH
OH
OH
Al
CH3
CH3
CH3
A)
B)
OH
Al(CH3)3
OH
OH
Trimethyl Aluminum
(TMA)
CH4
Al
CH3
Al
CH3
CH3
H2O
Al
CH3
CH3
CH3
OH
OH
OH
Al
CH3
Al
CH3
CH3
Al
CH3
CH3
CH3
CH3
OH
OH
OH
Al
Al
CH3
CH3
H2O
H2O
OH
CH4
OH
OH
Binary Reaction Sequence for Al2O3 ALD
1 ALD Cycle of TMA/H2O Deposits 1 Al2O3 “Monolayer”
Courtesy from J. W. Elam
Notes: 8
Growth rate (“Monolayer” thickness) is governed by steric hindrance of ligands remaining on surface following metal precursor exposure

## Slide 9
Courtesy from J. W. Elam
Notes: 9

## Slide 10: What ALD Capable of Engineering MCPs
Tuning resistivity of Materials
Tuning thickness of Materials
Tuning SEY coefficient of Materials
Courtesy from J. W. Elam
A. U. Mane, Slade J. Jokela

## Slide 11: MCP with Pore Size from 6um to 1um
Atomic layer deposition is perfect for functionalizing channels with small pore size
Conductive coating
(thermal evaporation)
pore
S.M. George, Chem. Rev., 110, 111, 2011
J. W. Elam, Rev. Sci. Instru. Vol 73, 2981, 2002
Resistive coating (ALD)
Emissive coating (ALD)

## Slide 12: Engineering 1st strikes Two Discrete Structure at the Pore Entrance
Resistive layer
MCP substrate
ALD SEE layer
High SEE layer
by PVD
Electrode
End Spoiling

## Slide 13: How to control the depth of SEE into Pore by Physical vapor deposition
θ
The penetration depth depends on the θ
Bigger θ, Deeper the Penetration
The coating of High SEY layer tunable
θ1
θ

## Slide 14: Candidate Materials for High SEE
Materials with Negative electron affinity, including activated GaP, GaN, GaAs, Diamond, and such. Trade off (more dark events)
Diamond coating (SEE: <80)
Highly crystallized MgO by PVD process (SEE:<25)
MgO film
Single crystal MgO

## Slide 15: Engineering the SEE material inside of pore
High quality NaCl, CsI, MgF2, CaF2 (SEE 5-15)
ALD process exist for MgF2 and CaF2
ALD process can be developed for other candidate materials

## Slide 16: Decrease Ion Feedback of MCP
Ions produced inside of channel by electron collision between residue gas
He adsorption on surface could alleviate the ion feedback problem.
Optimizing surface chemistry could decrease ion feedback.
Ion Energy of Gas Molecules

## Slide 17: Conclusions
Timing of MCPs could be improved by:
  MCPs with smaller pore size
  Engineering the Pore Entrance
  Engineering the SEE material inside of pore
  Decrease Ion Feedback Effect
Surface modification techniques including ALD and PVD could have great impact on those aspects

## Slide 18: Supporting information
For L/D=60, V=1000kV,
  The existing electron has a median energy of 32.5 eV, an appreciate number of electron has energy >100eV
Ions produced inside of channel by electron collision between residue gas.
Nuclear instruments and methods, 162 (1979), 587-601.

## Slide 19: Components Contribute to Timing of MCP detector
V1
V2
V4
V3
V5
t1
t2
t3
t4
t5
Photocathode
Microchannel plate
Anode
Rev. Sci. Instrum. 81, 073112 (2010)
Vapp: Voltage applied through MCP.
L: MCP length
M: Number of MCP in the assembly.
m , e: electron mass and charge