## Slide 1: Ivan Bazarov
Fundamental processes in III-V photocathodes; application for high-brightness photoinjectors
Physics Department, Cornell University

## Slide 2: Contents
Motivation
NEA photoemission
Some practical aspects
Study cases: GaAs, GaAsP, GaN
Summary

## Slide 3: Why are we interested?
Photoinjectors: a photocathode in high electric field (>> MV/m), either DC or RF
Relativistic electrons can be further accelerated in a linac (linear accelerator) without degradation of beam brightness:
  CW ultra-bright x-ray sources; high power FELs
  Electron-ion colliders and ion coolers
  Ultrafast electron diffraction, etc.

## Slide 4: Energy recovery linac
Energy recovery linac: a new class of accelerators in active development
Essentially removes the average current limitation typical to linacs (i.e. Pbeam >> Pwall plug)
Average currents 10’s to 100’s of mA can be efficiently accelerated (and de-accelerated)

## Slide 5: Cathode figures of merit
QE and photon excitation wavelength
  E.g. 1W of 775 nm (Er-fiber /2) 6.2 mA/% 520 nm (Yb-fiber /2)  4.2 mA/% 266 nm (Nd-glass /4)  2.1 mA/%
Transversely cold (thermalized) electron distribution
  Directly sets the solid angle of the emitted electrons; an upper limit on achievable beam brightness

## Slide 6: Figures of merit (contd.)
Prompt response time
  A picosecond response is essential to take advantage of the space charge control via laser pulse shaping
Long lifetime and robustness
  Extraction of many 100’s to 1000’s of C between activations are necessary to make the accelerator practical

## Slide 7: Negative electron affinity
Defined as vacuum level Evac relative to the conduction band minimum
Negative affinity: the vacuum level lies below the CBM  very high QE possible
NEA:
  1) band bending
  2) dipole layer

## Slide 8: Strong p-doping
Alperovich et al., Phys. Rev. B 50 (1994) 5480: clean p-doped GaAs has Fermi level unpinned and shows little band bending
~1019 cm-3

## Slide 9: NEA: Cs ~monolayer
Cs was found to play a larger role for NEA instead: 1) band bending through donor surface states, and 2) dipole surface layer from polarized Cs adatoms
  Cs-induced donor-like surface states contribute their electrons to the bulk
  Hole depleted region (negatively charged acceptors) lead to band bending region
p-doped
bulk (neutral)
-
-
-
-
-
-
+
+
+
+
+
+
ionized Cs
bb region

## Slide 10: NEA: ~Cs monolayer (contd.)
Majority of Cs atoms become only polarized (not ionized), forming a dipole layer (e- Cs+)
GaAs
Egap = 1.42 eV
Before Cs
c = 4 eV
After Cs
ceff ~ -0.1 eV
Vbb ~ 0.4 eV
dbb ~ 10 nm

## Slide 11: Spicer’s magic window
(1) electron-electron scattering: typical of metals, large energy loss per collision
(2) electron-phonon scattering: slowly depletes excessive energy of excited electron (LO phonons in GaAs ~ 35 meV)
“Magic window”: in semiconductors, one needs excess KE > Egap for e–/e– scattering. Thus, electrons excited with Evac < KE < EVBM + 2Egap have excellent chances of escape
(1)
(2)

## Slide 12: Electron transport processes
CBM thermalization time: 0.1-1ps
Electron-hole recombination: ~ns
Emission time:  1/(a2D) strong wavelength dependence

## Slide 13: Energy vs. momentum

## Slide 14: Role of fluorine/oxygen
Routine “yo-yo” activation employs O2 or NF3
Further reduction of affinity consistent with a double dipole model
Stabilizes Cs on the surface; no lifetime or otherwise apparent advantage for either gas
Bonded unstable nitrogen is found on Cs-NF3 activated surfaces (APL 92, 241107)
Yo-Yo Activation
JAP 54 (1983) 1413

## Slide 15: GaAs: Optimal Cs coverage
Ugo Weigel, PhD thesis
laser wavelength: 670 nm

## Slide 16: Lifetime matters
H2O, CO2 and O2 can lead to chemical poisoning of the activated layer
Low current (~ 1mA) 1/e lifetimes ~ 100 hours typical in our prep chambers
3-5 times better in the DC gun (low 10-12 Torr vacuum)
High average current (mA’s) lifetime limited by ion backbombardment

## Slide 17: 14 mA
~5 hour lifetime (limited by gas backstreaming from the beam dump), i.e. 20 hours 1/e for 5 mA
10 min

## Slide 18: Study cases
Our group has been evaluating III-V photocathodes
  Transverse energy of electrons (thermal emittance)
  Measure the photoemission response time
Materials studied so far
  GaAs @ 450-850nm: JAP 103, 054901; PRST-AB 11, 040702
  GaAsP @ 450-640nm: Ibid
  GaN @ 260nm: JAP 105, 083715

## Slide 19: Diffusion model
subject to:

## Slide 20: GaAs absorption
response time expected to scale as a–2 with wavelength (a lot!)

## Slide 21: Prompt emitters
deflector off
GaAs @ 520 nm
Measurements done by transverse deflecting RF cavity
Limited by 1.8 ps rms resolution dominated by laser to RF synchronization
GaN @ 260 nm

## Slide 22: Diffusion tail
P concentration 45%
Strong QE dependency
Two valleys: G (direct) and X (indirect) involved in the process
GaAsP @ 520 nm

## Slide 23: Transverse energy distributions
No surprises for bulk GaAs: cold electrons with a near band-gap excitation
GaAs
Surprisingly large transverse energy spread for GaN and GaAsP:
  GaAsP: kT = 130-240 meV for photons 0-780 meV photons above the band-gap
  GaN: kT = 0.9 eV for photons with 1.4 eV above the band-gap

## Slide 24: Summary
Transverse energy of photoelectrons remain poorly understood for III-V semiconductors (other than GaAs)
More carefully controlled experimental data on transverse energy distributions/time response needed
Predictive codes and models need to be developed and benchmarked with experiments
This will allow photocathode engineering with the desired characteristics such as cold electrons with a ps response

## Slide 25: Acknowledgements
Bruce Dunham, Xianghong Liu, Yulin Li
Amir Dabiran (SVT)
Dimitry Orlov (Max Planck Institute NP)
Matt Virgo (ANL)